**Mar-Tek Industries, Inc.**

**Material and Construction for**

**UL & CSA RECOGNIZED PRODUCTS**

The following table identifies the component product listings for labels Mar-Tek Industries, Inc. has with **Underwriters Laboratories (UL)**.

# UL Listings:

# Indoor Use Labels

Mar-Tek Industries, Inc. file number with UL is #MH17536.

|  |  |
| --- | --- |
| **Listing Reference** | **Base Material / Construction** |
| P5-200 | White Polyester, 5 mil thickness with permanent adhesive back, top surface printed with 2 mil protective over laminate. |
| P2-200 | White Polyester, 2 mil thickness with permanent adhesive back, top surface printed with 2 mil protective over laminate. |
| P5-SG | White Polyester, 5 mil thickness with permanent adhesive back, top surface printed with screened matte/clear protective coating over top surface. |
| P5-SG2 | White Polyester, 5 mil thickness with permanent adhesive back, top surface printed with screened matte/clear protective coating over top surface computer printable. |
| Polycarbonate Label | 5 mil to 20 mil thick polycarbonates, sub surface printed, backed with 3M 200MP Series permanent adhesive. |
| Aluminum Label | 8 mil to 32 mil thick aluminum, top surface printed, backed with 3M 200MP Series permanent adhesive. |
| AL7-11-200 | 2 mil chrome polyester with 2 mil over laminate. |
| AL7-11-100 | 2 mil chrome polyester with 1 mil over laminate. |
| 300-MTI | 5 mil to 20 mil Polycarbonate with 3M 300LSE Adhesive |

# Indoor or Outdoor Use Labels

Mar-Tek Industries, Inc. file number with UL is #MH17536.

|  |  |
| --- | --- |
| **Listing Reference** | **Base Material / Construction** |
| P5-100 | White Polyester, 5 mil thickness with permanent adhesive back, top surface printed with 1 mil protective over laminate. |
| P2-100 | White Polyester, 2 mil thickness with permanent adhesive back, top surface printed with 1 mil protective over laminate. |
| SC-100 | White Vinyl, 2 mil thickness with permanent adhesive back, top surface printed with 1 mil protective overlaminate |
| SC-OPC | White Vinyl, 2 mil thickness with permanent adhesive back, top surface printed with screened clear protective coating over top surface. |

Rev 02/20/2019 Page 1 of 2

Outdoor Use Labels

Mar-Tek Industries, Inc. file number with UL is #MH17536.

|  |  |
| --- | --- |
| **Listing Reference** | **Base Material / Construction** |
| MTI-ODU1 | 5 mil to 20 mil thick polycarbonates, sub surface printed, backed with 3M 200MP Series permanent adhesive. |
| 3690ODU | 3M 3690 White with Nazdar 3500 Inks |

# CUL Listings (Certified for Canada)

Mar-Tek Industries, Inc. file number with UL is #MH17536.

|  |  |
| --- | --- |
| **Listing Reference** | **Base Material / Construction** |
| Polycarbonate Label | 5 mil to 20 mil thick polycarbonates, sub surface printed, backed with 3M 200MP Series permanent adhesive. |

**Canadian Standards Association**

# 

# USE: On Metal (max temp 100C), and Plastic Group III (max temp 80C).

# **CSA Listings**

Mar-Tek Industries, Inc. file number with CSA is #078585\_L\_000.

|  |  |
| --- | --- |
| **Listing Reference** | **Base Material / Construction** |
| Pressure-sensitive “DPM PWS”\*\* | 2 mil White polyester with Clear Polyester Lamination. Indoor Wet |
| Pressure-sensitive “#200-4986”\*\* | 2 mil Silver Polyester with Clear Polyester Lamination. Indoor Wet |
| Pressure-sensitive “#200-4986”\*\* | 2 mil Clear Polyester with Clear Polyester Lamination. Indoor |
| Pressure-sensitive “L-156”\*\* | 4 mil White Vinyl with Clear Polyester Lamination. Indoor Wet |
| Pressure-sensitive “468”\*\* | 5-20 mil Matte/Clear Polycarbonate with 3M 200 MP Series Adhesive. Indoor Wet |
| Pressure-sensitive “468”\*\* | 5-20 mil Velvet Matte/Clear Polycarbonate with 3M 200 MP Series Adhesive. Indoor Wet |
| Pressure-sensitive “7033-350”\*\* | 3 mil Silver Polyester with Clear or Matte Polyester Lamination. Indoor / Outdoor |
| Pressure-sensitive “7872-350”\*\* | 4 mil Platinum Polyester with Clear or Matte Polyester Lamination. Indoor / Outdoor |

Rev 02/20/2019 Page 2 of 2